## Slide 1: Bias Fields and Pattern Complexity
M.E. Glicksman
Allen S. Henry Professor of Engineering
Mechanical & Aerospace Engineering Dept.
Florida Institute of Technology, Melbourne, FL
Presentation at the UCLA Institute for Pure & Applied Mathematics
Los Angeles, CA
November 13, 2012

## Slide 2: Outline
Pattern formation & microstructures
Early experiments & conventional ideas
Surprises from microgravity experiments
Conservation of energy
Capillarity, more than a boundary condition!
Bias fields: Why did we miss it?
Dynamic simulations

## Slide 3: Motivation & Associated Questions
Complex pattern evolution occurs throughout nature, society, and technology.
Self-organized patterns remain important in areas as diverse as cosmology, meteorology, biology, and engineering.
Branching (ramification and splitting) allows simple starting forms to achieve increasing complexity.
Is there a causal principle responsible for branching and surface diffusion?
Where does the information driving complexity reside ?
Is pattern branching fundamentally stochastic or deterministic ?

## Slide 4: Self-Organized Branching Patterns
Dendritic Photonic Array
Dendritic Superalloy
Morpho Retenor
Polycrystal
Directional
Monocrystal
Bio-iridescence
Electro-magnetic diffraction
Photonic (chiten) dendrites
Sensitive chemical probes
Pigmentless paints & coatings
Turbine blades
Jet engine efficiency
Microstructure control
Mechanical properties
Improved creep resistance

## Slide 5: Phase-Field Simulated Cu-Au Dendrite Courtesy of J. Warren & W. Boettinger, NIST
• Noise is considered essential—??
• Modelers unaware of a basic mechanism
• Sophisticated modeling—but:
• Pattern optimization & control limited
• Missing link is the interface ‘bias field’

## Slide 6: Pattern Evolution
‘Seaweed’: Fluid-fluid penetration, Hele-Shaw patterns, petroleum recovery, biogenesis
Dendrites: Casting, welding, primary metals production, crystal growth
What’s causal?

## Slide 7
Pattern Size & Supercooling
7-9s SCN
ΔT=6.82 K
V= 3.65 cm/s
ΔT=4.61 K
V= 1.25 cm/s
ΔT=4.00 K
V= 0.86 cm/s
ΔT=3.00 K
V= 0.38 cm/s
ΔT=2.00 K
V= 0.14 cm/s
ΔT=1.25 K
V= 0.032 cm/s
40 micron
• Solid-liquid interface is a source of heat/solute
• Energy/solute released must be transported away
• Boundary conditions: capillarity, kinetics, and T
• Branches appear periodically, develop irregularities
• Noise and stability responsible for pattern formation.

## Slide 8: NASA Microgravity Experiments
IDGE Experiments
Field Theory
Numerics
Bias Field Analysis
Dynamic simulation
Conclusions
Melting
Solidification
Provided the big clue
on pattern formation!

## Slide 9
IDGE

## Slide 10
USMP-4/IDGE Space Flight Instrument
Precision thermostat: (0.002 K)
Xenon flash
35mm camera
CCD camera
Sample chamber
Red LED

## Slide 11
Dendritic Growth in Space
(PVA, ΔT=1.2K)

## Slide 12: Melting PVA Dendrites (ΔT=1.8 K)

## Slide 13: C/A Measurement

## Slide 14: Analysis of Melting in Microgravity
Field Theory—a few words
  Coordinate system
  Laplace field
  Origin of self-similarity
  Melting kinetics

## Slide 15
Confocal Prolate Spheroidal Coordinates
=0
=1
0.9
0.75
0.5
0
0.25
1.1
1.3
1.6
=2
=-1
-0.9
-0.75
-0.5
-0.25
1
1.03
C/A=20
A. Lupulescu, M.E. Glicksman, and M.B. Koss,
J. Thermophysics and Heat Transfer, 17, (2002)
Exterior potential
Interior potential

## Slide 16: Self-Similar Melting (9:1Ellipsoid)
C/A
time
Self-similarity
Vector gradient fields: Isothermal interface

## Slide 17: Melting ‘Trajectory’ (St+ =0.036, C/A=15, C0 =0.76cm, Ξ=1.0026)

## Slide 18: C/A versus Time: Big surprise!
Self-similar
?
Not self-similar

## Slide 19
Self-similarity
TTTTint =const.
Numerical (Finite Difference)
no capillarity, Dr. S. Salon, RPI
  Gibbs-Thomson bc imposed
  Tint now depends on curvature, κ
  We found:
  • Interior heat flow
  • Capillary-mediated fluxes
  • Non self-similar melting!
≥
TTTTint ≠ const.

## Slide 20: Excess Flux

## Slide 21
Gibbs-Thomson-Herring Potential
Convex Gamma Plots
isotropic
anisotropic
Avoids equilibrium facets

## Slide 22: Global vs. Local Thermodynamic Equilibrium
Global equilibrium: Strong condition that minimizes Gibbs free energy
Local equilibrium: Weak condition that reduces free energy
in open systems
in closed systems
Allow dynamics:
Allow dynamics:
Initial state
Initial state
equilibrium
equilibrium
bias field
bias field

## Slide 23: Energy Conservation 2-Phase Domain Contraction
c
D(t)
N
S(t)
n
Domain
Contraction
S(t)
n

## Slide 24: Interface Energy Conservation (Leibniz-Reynolds & Kelvin-Stokes thms)
(Domain contraction)
(Fourier’s law )
(Local equilibrium)
(Meso-scale)
c
D(t)
N
S(t)
n

## Slide 25: Interface Energy Conservation
Definitions
Bias Field Modulation
Interface Poisson Eqn.
Ref.
Mod.

## Slide 26
ΔT=0.07 K
-------------
1000 μm
ΔT=0.37 K
-------------
125 μm
ΔT=1.00 K
------------------
50 μm
ΔT=1.35 K
--------------------
50 μm
Red line shows last discernible branch location.
Branch Initiation: A non-self similar event, suggesting a 2nd field!

## Slide 27: Capillary-mediated branching
Analysis: circle, ellipses, parabola, hyperbola, . . .
  Applied local equilibrium (GTH) on non-equilibrium analytic shapes
  Tangential interface fluxes
  Flux divergences
  Roots (sign change)
bias fields
advance/retard, Δvn
branching!
Stefan interface balance
modulation

## Slide 28: Initial Interface Shapes (Isometric Views)
a
Ellipse, 2:1
Circle, R=1
melt
melt
crystal
crystal

## Slide 29: GTH Potentials
Circle
Ellipse 2:1

## Slide 30: Tangential Fluxes
Circle
Ellipse 2:1

## Slide 31: Bias Fields
Circle
Ellipse 2:1

## Slide 32: Energetics & Dynamics
Simulation
  Integral eqn. solver
  Stefan interface balance
  Observed rotation points
  Pattern limit cycles

## Slide 33: Energy Conservation: Stefan balance
melt
crystal
Latent heat
Bias Field
Bulk energy conduction
Fast microscopic processes
Slow macroscopic processes
Interface modulation eqn:

## Slide 34: Bias Field Nodes
retard
advance
retard
advance
retard
retard
advance
advance

## Slide 35: Initial Bias Field & Patterns

## Slide 36: Circle Dendrite
(ε=0.005)

## Slide 37
1000 microns
ΔT=70 mK
Last discernible branch
Branch initiation
(estimated)

## Slide 38: Semi-ellipse
(ε=0.005)

## Slide 39: Bias Field Nodes, Ellipses (ε=0.005)

## Slide 40: Deterministic Chaos, ‘Seaweed’ (ε=0)

## Slide 41: Conclusions
Pattern complexities in iridescent butterfly wings and dendritic crystals are interesting and controlled branching provides technological applications.
Conventional wisdom attributes pattern branching to noise and stability.
NASA-supported microgravity experiments demonstrate that capillary potentials (local equilibria) provide weak interfacial fluxes.
Vector flux divergences imply energy release or removal (biases) on interface.
Nodes in the bias-field correspond to zeros of the surface Laplacian of the interface potential, a 4th-order function of the interface shape.
Positive bias energy retards interface speed, negative bias accelerates it.
Local changes in interface curvature couple with the external field and produce branching.
Synchronization of bias nodes with interface advance can lead to limit cycles, and dendritic growth if anisotropy is present.
Isotropic (fluid-fluid) interfaces evolve by chaotic dynamics, yielding complex ‘seaweed’ patterns.

## Slide 42: Acknowledgments
Special thanks go to Professors John Lowengrub, Mathematics Dept., U. California, Irvine, CA, and Shuwang Li, Dept. of Applied Mathematics, IIT, Chicago, IL for their efforts in providing noise-free sharp interface dynamics proving the existence of local bias fields.
Thank you for listening!